DANYANG YONGHE EIECTRIC TECHNOIOGY CO.,LTD

Aluminum Based Copper Foil Laminate Properties

| Item | Test condition | Index |
| --- | --- | --- |
|  |  | YH-01 | YH-02 | YH-03 |
| (W/m.k) Thermal Conductivity | A | 1.0 | 1.5 | 2.0 |
| (N/mm) Peel Strength | A After thermal stress | ≥1.8 | ≥1.8 | ≥1.8 |
| Blister test After Thermal stress | A After thermal impact | 260℃2min | 288℃ 2min | 300℃ 2min |
| Flammability | UL94 | V-0 | V-0 | V-0 |
| (℃/W) Thermal resistance max | A | ≤1.2 | ≤1.0 | ≤0.75 |
| (MΩ.m) Surface Resistance | A Constant humidity treatment (90%, 35 ℃,96H) | ≥1×105 | ≥1×105 | ≥1×106 |
| (MΩ.m) Volume Resistively | A (90%,35 ℃,96H) | ≥1.8×106 | ≥1.8×106 | ≥1.8×107 |
| (KV)min Dielectric Breakdown | A | ≥2.0 | ≥2.5 | ≥3.0 |
| (1MHz) Dielectic Constant | (40 ℃,90%,96H) | ≤4.4 | ≤3 | ≤2.5 |
| Dissipation Factor | (40 ℃,90%,96H) | ≤0.03 | ≤0.03 | ≤0.03 |

(Remarks)：

Product Material Description: 1060-type aluminum，

3003-type aluminum, 5052-type aluminum

copper foil: Japanese Import

2.ISO9001：2000，（UL：E333095）

Qualification Certificate: ISO9001: 2008 quality certification, SGS environmental protection  Certification,UL Safety Certified (UL NO.: E333095)